## Slide 1: Durability Assessment of Large Surfaces Using Standard Reliability Methods
M. Sykora & M. Holicky
Czech Technical University in Prague
Introduction
Measurements
Simplified deterioration model
Example
Conclusions

## Slide 2: Cooling tower and its maintenance

## Slide 3: Steel retaining walls

## Slide 4: Site measurements Local distribution of a carbonation depth
spatial variation (environmental actions, material properties)? → discretisation techniques → simplified approach based on “independent” elementary surfaces

## Slide 5: Simplified deterioration model
- division into zones (similar exposures – splash/upper parts of piers)
- within zones homogeneous random fields W (material properties, concrete cover) + hyperparameters X (single value for whole structure)
discretization of the zone into N elementary surfaces (random field variables independent)
fib Bulletin 59 Condition control and assessment of reinforced concrete structures

## Slide 6: Simplified deterioration model
Pf(t) = P{ndeg(t) / N ≥ alim} = EX(t){1 - Fbinom[Nalim, N, pf(W|x(t))]}
- For steel structures the size of an elementary surface may correspond to a size of inspected areas (e.g. 3 m)
- Concrete, chloride ingress ~ 0,5-2 m
The limiting deterioration level alim = 0,1-0,2
alim = 0,15 accepted in the example
pf(∙) is the failure probability of an elementary surface
FORM/ SORM

## Slide 7: Example – carbonation of concrete fib Model Code for Service Life Design
elementary surface: pf(t,mR|kS,x) = P[R(mR) − kS S(t,W|x) < 0]
Measurements
no trend?

## Slide 8: Variation of Pf(t) with t R = 25 mm, alim = 0.15

## Slide 9: Probabilistic optimization of the concrete cover
The total cost
Ctot = C0 + C1 μR + E[Cf]
Expected consequences
Annual discount rate q

## Slide 10: Variation of optimum reliability index bopt with N q = 0.03, t = 40 years, and Cf / C1 = 100 and 1 000

## Slide 11: Conclusions
Structural durability may be affected by spatial variability particularly for large surfaces.
Presented model seems to require lower computational demands compared to random field techniques (to be proved by upcoming studies).
This model is expected to be an effective tool for optimisation studies.
Numerical example of concrete carbonation reveals that the failure probability somewhat increases with a size of surface.
The optimum concrete cover and reliability index can be considered independent of the size of the surface area.

## Slide 12
Miroslav Sykora and Milan Holicky miroslav.sykora@klok.cvut.cz
Durability Assessment of Large Surfaces
Using Standard Reliability Methods
Thank you for your attention.

## Slide 13: Concrete Cover (cooling tower EDUV5)